## Slide 1: Integrated energy micro-storage
David Pech
dpech@laas.fr
Notes: Good morning… My name is D. Pech, I’m a CNRS Researcher at LAAS-CNRS and I am happy to give you today an overview of my research activities on … micro-batteries and -SC. And will mainly focus here on new these components called -SC.

## Slide 2: Context: Self-Powered Applications
Power
Management
Energy
Harvesting
Sensor
Data
Transmitter
Energy
Storage
Autonomous Embedded Microsystems:
Wearable Electronics, WSN, IoT.
 | MICRO-BATTERIES | Micro-Supercapacitors
Power | Low | Ultrahigh
Lifetime | Low | Almost unlimited
Energy | High | Low
Notes: Today, increasing need for …
These networks control hundreds of autonomous microsensors deployed over an area (èria) of interest. They collect, process and transmit local data to the network. A critical requirement for these small sensors nodes is energy autonomy. Power can be extracted by harvesting energy from the environment (light, heat, wind, mechanical vibrations), but this energy is not always available
This energy is recovered intermittently.
Requires an energy-storage component to ensure an energetic self-sufficiency over long periods of time.
Micro-battery
Is also -SC
POWER : What does it mean ? it can uptake or deliver a quantity of energy in very short times…
LIFETIME : (some -SCs can sustain millions of cycles of charge/discharge)
ENERGY : However a microSC cannot store a large amount of energy

## Slide 3: What is a micro-supercapacitor ?
D. Pech, C. Lethien, T. Brousse,
Techn. Ing. vol. RE180 (2017).
Notes: Just like a micro-battery, a -SC is miniaturized… rechargeable… energy storage… component.
and it consists of a positive and a negative electrode separated by an ionic conductor electrolyte.
2 configurations
Gravimetric / volumetric property

## Slide 4: Technological processes
INNOVATIVE ACTIVE MATERIALS
Activated Carbon, Carbon Nanotubes,
Onion-Like-Carbon, Carbon Nanowalls,
Carbide Derived Carbon, RuO2, MnO2,
Si Nanotrees, Si Nanowires,
Li4Ti5O12, Li2Mn3NiO8, LiFePO4…
A. Kyeremateng, T. Brousse, D. Pech,
Nat. Nanotechnol. vol. 12, p. 7 (2017).
Notes: Various micro-fabrication methods have been investigated at LAAS-CNRS to realize energy-storage micro-devices patterned with submillimeter-scale features.
* The challenge is to obtain the electrode material locally onto the microsized patterns without shorting the positive and negative electrodes
* Has to be compatible with the ones employed in the semiconductor industry.

## Slide 5: Energy Performance
Thin-film
micro-SC
Areal energy still far
for self-powered applications…
Notes: Results obtained between 2010 – 2016 for different µ-SCs based on different materials obtained via different technologies.
Our results + from literature
Areal Capa
Major advances : du µF au … mF/cm2
However (2s), emerging field of research /no proper benchmarking standard is currently available
Macro SC : FAR from the properties of bulky electrodes  (mJ / J) unable to power sensor or electronic component

## Slide 6: How to increase the areal energy ?
3D: a way to increase the quantity of active material per surface area
Notes: So how can we drastically (dras-tikly) increase the areal (èrial) energy of micro-SC ? Well, an interesting approach is to move from a 2D to a 3D electrode architecture.
Using a 3D architecture, for same footprint area, much much higher developed surface area
Quantity of active material per … : 1) et 2)

## Slide 7: Porous current collectors
Notes: That’s what we did : we created highly porous current collectors using an ingenious (injinious) electrodeposition technique.
The idea is to simultaneously generate hydrogen bubbles, under cathodic overpotential, and the electrodeposition of a metallic film. The bubbles shape the metallic film with porous, high surface area (èria)
over a broad range of pore sizes.
From the CV (electrochemical signature of the material)  EASA
To date, we can obtain an extended surface area (è-ria) exceeding 1000 cm2 for 1 cm2 of electrode.

## Slide 8: + RuO2 electrodeposition
A. Ferris, S. Garbarino, D. Guay, D. Pech,
Adv. Mater. vol. 27, p. 6625 (2015).
Highest value ever reported
(> 1 J/cm2, close to micro-batteries)
High cyclability, High power.
Notes: If we measure C, we get a value which exceeds – for the first time –1 F/cm2.
Breakthrough compare with state-of-the-art
but with much higher power and much higher lifetime

## Slide 9: From the material to the micro-device
2D MICRO-
SUPERCAPACITORS

## Slide 10: Conclusions
Per-area performance critical
(absence of standardized approaches)
Areal energy still far for self-powered applications
Need of a 3D paradigm shift for high-performance
micro-supercapacitors

## Slide 11: Funding Acknowledgment
ERC, Consolidator Grant, ERC-2017-CoG, Project 771793 3D-CAP